## Slide 1: Ionic crosslinking of cellulose nanocrystals
Han Chan, John Simonsen, John Nairn
Oregon State University

## Slide 2: Outline
Much ado about percolation
What is it?
Literature reports
Nairn Model
Ionic crosslinking
Testing the hypothesis

## Slide 3: PERCOLATION

## Slide 9
PERCOLATION!

## Slide 10
Garboczi, et. al. Phys. Rev. Ltrs. E, 1995, 52(1): 819-828
Aspect ratio = 70
Percolation threshold ~ 1%
Monte Carlo simulation

## Slide 11: Electrical conductivity
Alvarez, et al., J. App. Poly. Sci., (2006) 99:3005-3008

## Slide 12
Favier, et al., Poly. Eng. Sci. 1995, 37(10), 1735

## Slide 13: Battery Separator, CNCs in poly(ethylene oxide)
M. Samir, F. Alloin, J-Y Sanchez, A. Dufresne, 2004. Macromol. 37:4839-4844
Fuel cell operating temp

## Slide 14
Capadona, et al. Science 319 (2008) 1370
Enormous modulus loss on soaking in aqueous solution
Effective loss of percolation

## Slide 15: Shape-Memory effect
Mendez, et al. Macromol. 2011, 44, 6827

## Slide 16
Shape-Memory effect
Self-propelled fishing lure
Mendez, et al. Macromol. 2011, 44, 6827

## Slide 17
Faria, et al. J. Reinf. Plas. Comp. 2011, 30(20), 1729
A general problem for composites

## Slide 18
Muthirakkal, et al. Iran. Poly. J. 2010, 19(2), 89
A general problem for composites

## Slide 19: Carbon fiber has the same issue
Yu, et al. Polymer Composites, 2009, 1458
Pultruded vinyl ester-carbon fiber reinforced composite
Interlaminar shear stress

## Slide 20: Glass fiber in nylon
Hassan, et al. J. Reinf. Plas. Comp. 2011, 30(6), 488
As fiber content increases degradation of properties increases upon exposure to water

## Slide 21: Susceptibility to moisture
Most fiber-filled composites are susceptible to moisture intrusion
The interphase appears to be adversely affected by moisture intrusion
This is not a percolation effect, it is an interphase effect

## Slide 22: The Nairn model vs. The percolation model

## Slide 23: Use Model to Interpret Experiments
Experiments greatly exceed “expectation” from mean-field modeling
Experiments explained by
“percolation” which is a
nano phenomenon
Favier et al. (1995)
Great reinforcement
of the matrix
(>1000X)
Mean Field (2D, Halpin-Kardos)
Slide courtesy of Prof. John Nairn, OSU

## Slide 24: Alternate View: Use Better Mean Field
Mean Field (2D, Halpin-Kardos)
Experiments greatly exceed
“expectation” from mean-field
modeling
X
Favier et al. (1995)
Slide courtesy of Prof. John Nairn, OSU

## Slide 25: Alternate View: Interface vs. Percolation
Experiments explained by
“percolation” which is a
nano phenomenon
X
Favier et al. (1995)
“Modulus Percolation” - Ec increases slowly at first and then faster
Consequence of micromechanics and not of connectivity
Slide courtesy of Prof. John Nairn, OSU

## Slide 26: Alternate View: Ec/Em is Misleading
Favier et al. (1995)
Fiber reinforcement effects should be characterized by Ec - Em and not Ec/Em
Favier et al. (1995)
Great reinforcement
of the matrix
(>1000X)
X
Slide courtesy of Prof. John Nairn, OSU

## Slide 27: More comparisons
Chart: Volume fraction of filler, %
| 0 | 5.8999999999999995 | 11.799999999999999 | 17.7 | 23.599999999999998
PVDFHFP | 0 | 386.27 | 731.95 | 1651.675 | 2643.475
PVOH/0 PAA | 0 | 640 | 330
PVOH/10 PAA | 0 | 646 | 390
PVOH/20 PAA | 0 | 420 | 230
EO-EPI Capadona 2008 | 0 | 2 | 74 | 194 | 494 | 794
PVAc Capadona 2008 | 0 | 1 | 58 | 298 | 398 | 798
Styrenic acrylate Favier 1995 | 0 | 0.13643 | 1.5218 | 9.9369 | 63.0326 | 251.1255 | 316.1647

## Slide 28: Is it percolation or is it a bad interphase?
Or both?.....

## Slide 29
If only percolation changes, then no change in modulus
If only interphase changes, modulus will change about the same as uncrosslinked composite
If matrix also changes, properties will change, but less than unfilled control
Hypothesis: If the CNCs are crosslinked in a way that does not respond to water, then exposure to water should not reduce the modulus

## Slide 30: Ionic crosslinking
Form a CNC gel, “aquagel,” in water
Dry using supercritical CO2
Infuse the aerogel with polymer solution
  3D spatial distribution
Evaporate solvent
Test composite wet and dry

## Slide 31: Cellulose nanocrystals
Nanocel™
One step process
Can use a variety of biomass raw materials
Biomass
(NH4)2S2O8
pH 1
60 – 80 °C
16 h
CNCs + waste
C.CNCs
diafiltration
Bio Vision technology, inc.
~0.5 mmol/g CO2H
WO 2011072365, Mar 15, 2010

## Slide 32
0
5μm
0
5 μm
2 μm
Bio Vision technology, inc.
Slide courtesy of Bio Vision Tech. Inc.
Nanocel™

## Slide 33: Ionic crosslinking: Aquagel formation
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
CO2
M3+
M3+
M3+
M3+
M = Al3+, Fe3+, Zr4+, Dy3+

## Slide 34: Rapid Gelation
CNC solution
Add Fe(NO3)3
Aquagel

## Slide 35
decant
A low density aquagel

## Slide 36
Iron crosslinked CNC aquagel

## Slide 37: Iron crosslinked CNC aerogel

## Slide 38
10 nm

## Slide 40
No Fe
Fe present

## Slide 41: Sample prep
Form aquagel
Transfer solvent to acetone
Transfer to PVAc solution (10%)
Dry carefully
Test via compression for bulk modulus

## Slide 42: Preliminary data suggests interphase is more important!
Chart: Effective bulk modulus. g/mm
| Dy-C.CNC dry | Dy-C.CNC wet | C.CNC control dry | C.CNC control wet
 | 20203.5 | 4344 | 1578 | 1398

## Slide 43: Questions?